## Slide 1: NCAT Pavement Test Track
Welcome to the
5/11/11 Track Sponsor Meeting
The meeting will begin at 7:30 central time

## Slide 2: Morning Agenda
Operations & field performance by Buzz Powell
Structural performance update by Dave Timm
Break
Durability of PFC Surfaces by Don Watson
Ground Tire Rubber Modified Binder by Nam Tran
Lab to Field Comparisons by Buzz Powell
Planning for the 2012 Track by Buzz Powell

## Slide 3: Track Operations

## Slide 4: Trucking Operations

## Slide 5: Trucking Operations

## Slide 6: Trucking Operations12/6/2010

## Slide 7: Field Performance Update

## Slide 8: PFC Surface Cracks (Tack Method)
2006 crack susceptible dense Superpave mix
  Surface cracks after 1.9M ESALs (Rehab at 5.6M)
2009 PFC surface placed with conventional tack
  Surface cracks after 2.2M (cracking/pumping at 8.2M)
2009 bonded PFC surface placed with spray paver
  Surface cracks after 4.1M (looks pretty good at 8.2M)

## Slide 9: Cracking in Conventional Tack PFC

## Slide 10: Same Mix Drains Better at 1¼”
N1 - ¾”
Bonded
N2 - ¾”
Tacked
S8 - 1¼”
Tacked

## Slide 11: Thin Perpetual Pavements (N3/N4)

## Slide 12: 2009 Group Experiment (+)

## Slide 13: 2009 Group Experiment (+)

## Slide 14: Perpetual Pavement on Soft Clay

## Slide 15: High Polymer Inlay Still Looks Good3.6M ESALs

## Slide 16: N12 SMA with High F&E Aggregates

## Slide 17: Location of High RAP Test Sections
W3-20-76
W4-20-67
W5-45-52
E5-45-67
E6-45-76
E7-45-76s

## Slide 18: Location of High RAP Test Sections
N10–50-67
N11–50-67
S2-45-67
W3-20-76
W4-20-67
W5-45-52
E5-45-67
E6-45-76
E7-45-76s
S9-0-76

## Slide 19: 2006 High RAP Macrotexture

## Slide 20: 2006 High RAP Cracking

## Slide 21: 2006 High RAP Cracking

## Slide 22: W6 Pavement Preservation 4.75 Mix

## Slide 23: W8 & W9 High Friction Epoxy Surfaces
Taconite
Flint
Chinese bauxite
Silica
Granite
Basalt
Australian glass
Steel slag
Copper slag

## Slide 24: S2 High RAP Reflective Cracking

## Slide 25: S2 High RAP Reflective Cracking

## Slide 26: Raveling in Mississippi Mixes

## Slide 27: GTR vs SBS Modified Polymer Mix

## Slide 28: S13 Surface Treatment Cracking

## Slide 29: Profiler Certification Program

## Slide 30: National WMA Certification Program
9.5 mm coarse granite PG67-22 mix (TSR ≈ 0.3!)
Laboratory performance of plant produced mix
  Flow number, dynamic modulus, APA
  IDT, overlay tester, bond strength, PG grading
  TSR, stripping via boiling, Hamburg (aged & unaged)
Field performance on Pavement Test Track
  Hot-mix control, immediate traffic (1 year thereafter)
  Weekly rutting, roughness, macrotexture
  Final report within 18 months of commitment

## Slide 31: Interim WMA Field Results

## Slide 32: www.pavetrack.com
Home Sponsors Construction Trucking Performance Map to Track

## Slide 33: Web Performance Reports

## Slide 34: Questions ?