## Slide 1
Optimizing the Durability and Functionality of PFC Surfaces
Don Watson
Test Track Sponsor Meeting
May 11, 2011
Notes: 1

## Slide 2: Objective
Durability Issues
  Raveling
  Crack Resistance
Functionality Issues
  Permeability
  Smoothness
  Structural Value
Notes: Asphalt Technology Course
Introduction
2

## Slide 3
  Raveling
  Crack Resistance
Durability Issues
Notes: Asphalt Technology Course
Introduction
3

## Slide 4
Raveling

## Slide 5: Change in Texture with Traffic

## Slide 6: Crack Resistance

## Slide 7: PFC Surface Cracks (Tack Method)
2006 crack susceptible dense Superpave mix
  Surface cracks after 1.9M ESALs (Rehab at 5.6M)
2009 PFC surface placed with conventional tack
  Surface cracks after 2.2M (cracking/pumping at 8.2M)
2009 bonded PFC surface placed with spray paver
  Surface cracks after 4.1M (looks good at 8.2M)

## Slide 8: OGFC Surface Cracks (Tack Method)
Conventional Tack
Bonded

## Slide 9: 5/2/2011 Crack Maps (N2 / N1)

## Slide 10
  Permeability
  Smoothness
  Structural Value
Functionality Issues
Notes: Asphalt Technology Course
Introduction
10

## Slide 11: Permeability

## Slide 12: Same Mix Drains Better at 1¼”
N1 - ¾”
Bonded
N2 - ¾”
Tacked
S8 - 1¼”
Tacked

## Slide 13: Smoothness

## Slide 14: Change in Smoothness with Traffic

## Slide 15: Structural Value

## Slide 16: Structural Contribution of OGFC

## Slide 17: Similar Rutting Performance

## Slide 18: Similar Strain Response
50% RAP
Virgin Mixes

## Slide 19
Questions??
Notes: Asphalt Technology Course
Introduction
19