## Slide 1: Use of Ground Tire Rubber Modified Binder
Nam Tran
Lead Research Engineer

## Slide 2: Overview
Methods of incorporating GTR
Applications of rubber-modified binders
Performance of test sections at NCAT test track
Questions and concerns

## Slide 3: Methods

## Slide 4: Methods
Two methods for incorporating GTR into HMA
  Wet process
    GTR acts as a binder modifier (up to 20% of total binder)
    2 processes: asphalt-rubber and terminal blend
  Dry process
    GTR acts as a rubber aggregate (1-3% of aggregate)

## Slide 5: Asphalt-Rubber
> 15% crumb rubber passing #8 or #10 mesh
  Reacted sufficiently to cause swelling of rubber
2 types of asphalt-rubber binders
  Type I (used in AZ and TX) 18-20% crumb rubber
  Type II (used in CA) about 20% rubber
    75% tire rubber and 25% natural rubber
    May include up to 6% heavy aromatic oils
  Both types blended at elevated temp (>350oF) in low shear system for at least 45 minutes

## Slide 6: Terminal Blend
5-20% crumb rubber passing #40 or #80 mesh
  Blended in refinery or stationary asphalt terminal with little or no agitation
  Can contain polymers
  All components heated over extended period of time to dissolve rubber particles
Used in Arizona, California, Florida, Texas, and several northeastern states

## Slide 7: Asphalt Rubber vs. Terminal Blend
Asphalt Rubber
Rubberized Asphalt Terminal Blend
1,500-2,500 centipoises at 375°F, extremely viscous
300-600 centipoises at 325°F, significantly less viscous than AR
Rubber Pavements Association

## Slide 8: Asphalt Rubber vs. Terminal Blend
Use more crumb rubber
Requires special equipment to produce
Longer documented history of performance
Mostly uses recipe specs
Not cost effective in small quantities
Cannot be PG graded
Use less crumb rubber
Does not require special equipment
Shorter documented history
Many are proprietary
Rubber usage more difficult to document
Can be PG graded

## Slide 9: Applications

## Slide 10: Applications
Asphalt Rubber Concrete Dense-Graded
  Terminal blend (most effective), Asphalt rubber
Asphalt Rubber Concrete Gap-Graded
  Asphalt rubber (most effective), terminal blend
Asphalt Rubber Concrete Open-Graded
  Asphalt rubber (most effective), terminal blend
Stress Absorbing Membrane Interlayer (SAMI)
Stress Absorbing Membrane (SAM)

## Slide 11: Caltrans Reduced Thickness Design Guideline
Developed in 1992 based on laboratory and long-term field data (two decades)
Uses a deflection based design method
Up to 50 % reduction in thickness compared to conventional AC design thickness
Over 1000 reduced thickness projects

## Slide 12: Major Rubber-Modified Asphalt Users
California
  ARSC (AR chip seal)
  SAMI-R
  RHMA-O
  RHMA-G
  RHMA-D
Florida
  ARMI (SAMI)
  GTR modified-OGFC (FC-5)
  GTR modified-DGFC
Texas
  AR Chip Seals
  AR Underseal (SAMI)
  CRM-PFC
  CRM-HMAC
Arizona
  SAM
  SAMI
  ARFC
  ARAC

## Slide 13
South Carolina
Florida
North Carolina
Washington, D.C.
Delaware
New Jersey
Connecticut
Rhode Island
Massachusetts
Maine
New Hampshire
Vermont
New York
Ohio
Kentucky
West Virginia
Pennsylvania
Indiana
Illinois
Iowa
Missouri
Arkansas
Tennessee
Georgia
Alabama
Mississippi
Louisiana
Texas
Oklahoma
Nebraska
Kansas
South Dakota
North Dakota
Virginia
New Mexico
Arizona
Colorado
Utah
Nevada
California
Alaska
Minnesota
Wisconsin
Michigan
Montana
Wyoming
Idaho
Oregon
Washington
Maryland
Hawaii
Rubber used
Not using rubber
States where Asphalt-Rubber has been used
(DOT, Transportation Authority, County or City)
Puerto Rico
Rubber Pavements Association

## Slide 14: Performance of Sections S6 & S7

## Slide 15: Surface Mixes in Sections S6 & S7
S6 (SBS-modified 76-22)
  Missouri 12.5 mm coarse
  Limestone/porph + 2%HL
  Pb: 5.4%
  Pbe: 4.5%
  Va: 4.5%
  VMA: 14.8%
  Field Density: 93.1%
  Thickness: 1.9 in.
S7 (GTR-modified 76-22)
  Missouri 12.5 mm coarse
  Limestone/porph + 2%HL
  Pb: 6.0%
  Pbe: 5.1%
  Va: 3.3%
  VMA: 15%
  Field Density: 93%
  Thickness: 1.7 in.

## Slide 16: Laboratory Testing
Binder testing
  Performance grading
  Multiple-Stress Creep-Recovery (MSCR) test
Mixture testing
  Moisture susceptibility -- TSR (AASHTO T 283)
  Mixture stiffness – E* (AASHTO TP 79, PP 61)
  Rutting resistance – APA (TP 63), Hamburg, Fn
  Cracking – IDT and Energy Ratio

## Slide 17: Binders
S6
  SBS-modified PG 76-22
  True grade: 76.6-26.3
  M 320: 76-22
S7
  GTR-modified 76-22
    Terminal blended
    Proprietary
  True grade: 81.7-25
  M 320: 76-22

## Slide 18: Moisture Susceptibility (TSR)
S6 (SBS-modified 76-22)
S7 (GTR-modified 76-22)

## Slide 19: Mixture Stiffness (E*)
Chart: Log Frequency, Hz
| -6 | -5.75 | -5.5 | -5.25 | -5 | -4.75 | -4.5 | -4.25 | -4 | -3.75 | -3.5 | -3.25 | -3 | -2.75 | -2.5 | -2.25 | -2 | -1.75 | -1.5 | -1.25 | -1 | -0.75 | -0.5 | -0.25 | 0 | 0.25 | 0.5 | 0.75 | 1 | 1.25 | 1.5 | 1.75 | 2 | 2.25 | 2.5 | 2.75 | 3 | 3.25 | 3.5 | 3.75 | 4 | 4.25 | 4.5 | 4.75 | 5 | 5.25 | 5.5 | 5.75 | 6
S6-Confined | 77.0961 | 79.1382 | 81.543 | 84.38 | 87.7329 | 91.7037 | 96.4162 | 102.0217 | 108.7047 | 116.6903 | 126.2535 | 137.7282 | 151.5187 | 168.1104 | 188.0796 | 212.1012 | 240.9499 | 275.4928 | 316.6691 | 365.4535 | 422.7995 | 489.5654 | 566.4245 | 653.77 | 751.6268 | 859.5858 | 976.7739 | 1101.8694 | 1233.1638 | 1368.6647 | 1506.2236 | 1643.6739 | 1778.9587 | 1910.2374 | 2035.9602 | 2154.9094 | 2266.2095 | 2369.3119 | 2463.9607 | 2550.1494 | 2628.0711 | 2698.0706 | 2760.6005 | 2816.1818 | 2865.3726 | 2908.7426 | 2946.854 | 2980.2479 | 3009.4349
S7-Confined | 67.6251 | 69.9395 | 72.6551 | 75.8479 | 79.6098 | 84.0522 | 89.3106 | 95.5494 | 102.9687 | 111.8111 | 122.3703 | 134.9998 | 150.122 | 168.2362 | 189.925 | 215.8559 | 246.7761 | 283.498 | 326.8722 | 377.7456 | 436.9054 | 505.0104 | 582.5155 | 669.5985 | 766.0983 | 871.4777 | 984.816 | 1104.8391 | 1229.9816 | 1358.4764 | 1488.4593 | 1618.0764 | 1745.5809 | 1869.413 | 1988.2544 | 2101.0591 | 2207.0604 | 2305.7595 | 2396.9003 | 2480.4356 | 2556.4899 | 2625.3214 | 2687.2866 | 2742.8092 | 2792.353 | 2836.4003 | 2875.4353 | 2909.9308 | 2940.3393
S6-Unconfined | 25.1282 | 26.7508 | 28.684 | 30.9963 | 33.7732 | 37.1218 | 41.1763 | 46.1049 | 52.1181 | 59.4782 | 68.5107 | 79.6155 | 93.2789 | 110.0835 | 130.7138 | 155.9558 | 186.6853 | 223.8428 | 268.3926 | 321.2641 | 383.2791 | 455.0698 | 536.9971 | 629.0807 | 730.952 | 841.8384 | 960.5845 | 1085.7083 | 1215.4854 | 1348.0511 | 1481.5074 | 1614.0238 | 1743.9216 | 1869.7369 | 1990.2595 | 2104.5501 | 2211.9364 | 2311.9964 | 2404.5303 | 2489.5267 | 2567.1282 | 2637.5961 | 2701.279 | 2758.585 | 2809.9579 | 2855.8583 | 2896.7484 | 2933.0803 | 2965.2884
S7-Unconfined | 19.4314 | 21.3378 | 23.6301 | 26.3982 | 29.7547 | 33.8405 | 38.8313 | 44.9456 | 52.453 | 61.6837 | 73.0374 | 86.9908 | 104.1029 | 125.0149 | 150.4431 | 181.1627 | 217.9796 | 261.6917 | 313.038 | 372.6407 | 440.9452 | 518.1635 | 604.23 | 698.7754 | 801.1235 | 910.3119 | 1025.1364 | 1144.2113 | 1266.0419 | 1389.0997 | 1511.8935 | 1633.0304 | 1751.2641 | 1865.5273 | 1974.9494 | 2078.8606 | 2176.7852 | 2268.4269 | 2353.6478 | 2432.4458 | 2504.9301 | 2571.2981 | 2631.8135 | 2686.787 | 2736.56 | 2781.4907 | 2821.9427 | 2858.2766 | 2890.8433

## Slide 20: Rutting Resistance (APA, 64oC)
Chart: Surface Mixes
| S6 (SBS) | S7 (GTR)
Manual | 1.41 | 1.37
Automatic | 1.04 | 1.55

## Slide 21: IDT (10, 0, -20oC)
S6
  Strength @ 10oC: 4,394,770 psi
  Critical cracking temperature: -24.4oC
    True PG of binder: 76.6-26.3
S7
  Strength @ 10oC: 4,667,902 psi
  Critical cracking temperature: -25oC
    True PG of binder: 81.7-25

## Slide 22: On-going Testing
Rutting and moisture damage resistance
  Flow number
  Hamburg
Cracking resistance
  Energy Ratio

## Slide 23: Field Performance (Rutting)
S6
S7

## Slide 24: Field Performance (Roughness)
S6
S7

## Slide 25: Questions, Concerns and Needs

## Slide 26: National and Regional Levels
PG grading of rubber modified asphalt
  FHWA binder ETG is working on a test method
Determining rubber content
  No proposed method
Use of GTR-modified asphalt with WMA
  Asphalt rubber
  Terminal blend

## Slide 27: National and Regional Levels
Recyclability of GTR-modified asphalt mixtures
Incorporating GTR-modified mixtures in mechanistic pavement designs
  E* predictive models
  Mechanistic and transfer models
  Can we save up to 50% in thickness compared to conventional AC design thickness?

## Slide 28: Regional and State Levels
What are your questions or concerns when specifying GTR-modified binder mixtures and/or accepting new GTR-blending technologies?